SECTION 02791 – ATHLETIC AND RECREATIONAL SURFACING SPECIFICATION –

One and three quarters (1.75”) inch thick, yielding a five (5’) foot fall rating.

PART 1- GENERAL

  - DESCRIPTION

All necessary material components and application information required to install the molded one and three-quarters (1.75”) inch thick “Pave-Land” series featuring the “dual-density” construction with the new “Button-Lock™” technology, composed of clean rubber granules, using the “Step-&-Repeat” &/or the “Running Bond” method of installation, gluing the interlocks, bolting them down, shall be by Unity Creations Ltd. / Unity Surfacing Systems or approved equal, either of which has been manufactured in the United States of America for a period of ten (10) or more years.

  - QUALITY ASSURANCE

- Qualifications – Manufacturer shall have manufactured and marketed this system in the United States of America for a period of ten (10) years, using clean rubber granules, that has been recycled here in the United States of America from tires and rubber derived from the same.

- Installation – Labor shall be completed by “certified” installers with five (5) years experience installing rubberized safety surfacing, flooring and paver products in the tile/mat/block form.  Installation instructions shall be provided by Unity Creations Ltd. / Unity Surfacing Systems.  Glue shall be applied to the “male” interlocks (both in the joint and on top of the joint) as well as to the “slot” where the “projection” will meet for product-to-product, interlock-to-interlock and slot-to-projection adhesion during the installation process – not afterwards. Additionally, glue shall be applied to the base (underside) of each unit being installed via product-to-sub base adhesion; Screw-bolts shall be applied through the male interlocks, and countersunk for additional strength and security.

* Base gluing (glue-down) and screw-bolts do not apply to rooftop installations. Glue being applied to the interlocks, both in the joint and on top of the joint, shall be maintained.

- Design & Detailing – The “Pave-Land series is one and three-quarters inch (1.75”) thick utilized in the safety zones under and around all areas, etc. as an impact absorbing resilient unitary rubberized safety surfacing, flooring and paver application. “Pave-Land” is designed to meet ANSI/FM, ADA, CPSC, ASTM and USGBC-LEED requirements.  Acceptable substrates and substitute systems are: concrete (cement), asphalt (blacktop). As well as: compacted crushed stone, RCA, stone blend (call for details and specs), wood decking, roofing membranes (call for details and specs), indoor flooring and surfacing systems that do not have stress cracks, Unity Creations, Ltd. / Unity Surfacing Systems shall approve other substrates. Conditions of all substrates with respect to structural performance shall be evaluated and approved by the certified applicator prior to installing the “Pave-Land” series using the “step-& repeat” system.

- Based on a “certified” installation, the Contractor shall furnish the manufacturer’s 10-Year Limited Warranty, prorated as outlined in the manufacturer’s warranty coverage plan prior to installation. If a “non-certified” installer is used for the installation of the safety surfacing material, or a warranty is not selected prior to installation, a 5-Year Limited Warranty, prorated as outlined in the manufacturer’s warranty coverage plan must be provided. This warranty may be transferred with the property.

  - SUBMITTALS

- Submit product information in the form of manufacturer’s technical data, specifications, installation instructions, repair & maintenance guide.

- Submit product samples showing the “Dual-Density” construction with each unit weighing a minimum of 35 pound (lbs) per unit or 5.20 pounds (lbs) per square foot,

- Submit product samples of unitary rubberized safety surfacing, flooring and pavers in the tile/mat/block form in all available colors. Including the EPDM granules in all colors and color blends available,

- Submit product samples showing both the “male” and “female” self-interlocking connection that is built directly within the product itself, showing the male connectors of the unit being engagable with the female receptacle of the adjacent unit so that they may interlock with themselves (i.e. without the assistance of an independent piece and/or item).

- Submit product samples showing the new “Button-Lock™” technology where the “projections” of a tile/mat/block (unit) are receivable by corresponding “slots” of the adjacent unit to help further strengthen the connection of the self-interlocking system.

- Submit product samples showing a glue reservoir on the back wall of the female receptacle where excess glue will escape downwardly through the channel formed in the inner wall of the female receptacle to the sub-base and away from the top of the tiles/mats/blocks (units).

- Submit product samples showing the bolt-down mechanism found within the “male” portion of the interlocking system where it is recessed and counter-sunk,

- Submit shop drawings showing layout of safety surfacing, flooring and pavers; include edge detail(s) of flush mount installation, cut paver detail(s), fastening detail and details at penetrations for playground equipment.

  - DELIVERY, STORAGE AND HANDLING

All materials shall be delivered in good condition in its original unopened packages, bound and shrink wrapped with labels intact.  All materials shall be protected from weather; and the adhesive (glue) shall be stored at temperatures of 40 degrees Fahrenheit (4 degrees Celsius) or greater.

  - JOB CONDITIONS

At the time of application ambient air temperature shall be 40 degrees Fahrenheit (4 degrees Celsius) or greater for a period of twenty-four (24) hours.  All materials shall be un-stacked and layed out prior to installing. Color blending may be necessary to achieve uniformity. All materials shall be protected from weather and other damage prior to application, during applications and while glue is curing.

PART II: PRODUCTS

2.01 GENERAL

All material components of the “Dual-Density” “Pave-Land” series with the new “Button-Lock™” technology shall be obtained from Unity Creations, Ltd. / Unity Surfacing Systems or its authorized distributors and / or manufacturers only.  Shall be manufactured in the United States of America, and meet standards specifications under the LEED (Leadership in Energy and Environmental Design) criteria developed by the USGBC (United States Green Building Council) establishing a minimum of seven (7) points / credits.

2.02 MATERIALS

- The architect and / or engineer, in writing, prior to bid date, shall approve any system or series, to be considered equal to “Pave-Land”. Samples of equal materials showing the self-interlocking connection with the new “Button-Lock™” technology and bolt-down capabilities, in all colors, must also be submitted prior to bid date.

Acceptable Manufacturer:

Sales & Marketing Dept:					Manufacturing Plant:

Unity Surfacing Systems 					Unity Creations, Ltd.

56 Bloomingdale Rd.						3997 RT 9W (PO Box 9)

Hicksville, NY. 11801					Saugerties, NY. 12477

T: (516) 724-1357						T: (845) 246-2700

F: (845) 246-1700						F: (845) 246-1700

E-mail: productinfo@surfacingsystems.com                       techinfo@surfacingsystems.com

Internet: www.surfacingsystems.com 		  Internet: www.surfacingsystems.com

- Unity Creations, Ltd. / Unity Surfacing Systems: tiles/mats/blocks shall be produced on a                                    rectangular configuration of 22” (inches) by 44” (inches) in size [+/- one-quarter (1/4”) tolerance] with a shadow-center (fake seam) joint to achieve the use of the “step-&-repeat” &/or the “Running Bond” method if installation to stagger (zigzag) the seams as if you were installing brickwork, lining real seam up with fake seams. As a result, symmetry of 22” by 22” squares will be seen on properly completed jobs (installations). Each tile-mat-block is 6.72 square feet in size [+/- one-quarter (1/4”) tolerance] and has a coned (feet &/or leg) bottom design. Thickness is one and three-quarters (1.75”) inch thick for the “Pave-Land” series to meet a five (5’) fall rating (please consult with the contractor, architect, and or, engineer to determine which thickness is needed based on drop height requirements).

- Shall be tested for shock attenuation under ASTM F 1292-04, G Max and HIC based on the thickness of material and/or drop height requirement needed.

- Shall also have the following technical qualifications:

  - TESTING

ASTM: American Standard for Testing Materials; CPSC: Consumer Product Safety Commission; ADA: Americans with Disabilities Act. USGBC: United States Green Build Council. LEED: Leadership in Energy and Environmental Design. ANSI: American National Standard Institute, FM: Factory Mutual.

Fall Safety Heights: ASTM F 1292-04, F-355-04. To meet a five (5’) foot fall rating;

Weathering (Aging): ASTM C-67, D-573, F1292-95. To meet a five (5’) foot fall rating;

Spread of Flames:  ASTM E108 Class A. ASTM E108 modified for roof coverings;

Spread of Flames:  ASTM E648 Class I: Minimum 0.45 watts/cm2;

Skid Resistance: ASTM 303-93; To measure and describe the slipperiness of the surface material.

ADA: ASTM F-1991-99. Standard Spec for Determination of Accessibility of Surface Systems under and Around Playground Equipment:;

R-Value: ASTM: C518-98. Thermal Conductivity; Minimum of 2.4

LEAD Content: CPSC-CH-E1002-08 via US Public Law 110-314 (HR 4040 act of 2008); Less then 300 ppm resulting in Lead Content that is not detectable.

Reflectance/SRI & Emittance: ASTM E903, E-891, E-1980 – Based on color selected by Architect.

Water Penetration: Storm Water Management / Sustainable Run-off via drain ability. Flow rate at body equals 6.34 gallons (24.01 liters) for every twenty-four (24) minutes. Flow rate at seams equals 9.25 gallons (35.00 liters) for every twenty (20) minutes.

USGBC: MR 4.1, MR 4.2, MR 5.1, MR 5.2, MR 2.1 & MR 2.2, EQ 4.1. Seven (7) LEED Points/Credits;

Pull Force: ANSI/FM 4474. Uplift Pull Test Procedure estimated to be at 277.5 psf (2:1 Factor of Safety)

Wind Resistance: ASTM D3161-09. Fan-Induced test method for air velocity of 150 MPH for two hours.

Impact Resistance Test: UL 2218, 2010. Class 4 Impact Resistance Test of Prepared Coverings.

The values shown represent current production laboratory taken tests, which may vary when field-tested.

Glue: “Unity’s: Chemrex 948 Urethane (glue), shall be a one-part binder, requiring no on site mixing. Excellent strength, tenacity and grab for male interlock-to-female interlock as well as product-to-sub base installations.

Bolts: “Unity’s Screw-Bolts” shall contain a weather-resistant beveled recess-able head to be counter-sunk through the interlock; shall be a length necessary to securely fasten the tile/mats/block to the solid sub-base material. Excellent strength and grab for product-to-sub base installations. DO NOT USE BOLTS ON ROOFTOP INSTALLATIONS.

Color: To be determined by architect/engineer from manufacturers list of at least eleven (11) pigmented choices and TPV/EPDM Blends.

PART III –EXCLUSIONS

3.01 INSPECTIONS

Prior to application of the Unity Creations, Ltd. / Unity Surfacing Systems “Pave-Land” series: the architect, engineer, municipality, general contractor, safety surfacing manufacturer and installer shall evaluate the substrate’s structural performance. Notify all contactors, architects and engineers of all displacements or stress cracks.  Work shall not proceed until unsatisfactory conditions are corrected and signed by the contractors, architects and engineers; And Unity’s installation manual/guide has been read.

  - INSTALLATIONS

Recessed installations are strongly encouraged to avoid the use of transitional ramps (edging). Contractor shall first install an approved solid sub-base material consisting of concrete (cement), asphalt (blacktop) or approved equal. Approved sub-base material shall extend three (3”) inches past the desired safety surfacing, flooring and paver zone of installation. Once cured, Unity Creations, Ltd. / Unity Surfacing Systems products shall be installed as specified. After completion of Unity Creations, Ltd. / Unity Surfacing Systems products, an approved boarding system consisting of concrete (cement), asphalt (blacktop) or approved equal shall be installed to be level/flush with the finished edge of the newly installed Unity Creations, Ltd. / Unity Surfacing Systems products. Said boarding system shall connect with the newly installed tiles/mats/blocks.

Please note: the height of the finished area (i.e. concrete walkway) and the sub-base material shall be consistent with the thickness of the tiles/mats/blocks/pavers being installed all the way around the entire area, prior to the installation of the safety surfacing materials. This shall be tested every 44” with a full size sample tile/mat/block given to the contractor prior to commencement of safety surfacing being installed. Contractor shall “certify” in writing that the test has been completed and verified with photographic images sent to the: architect, engineer, municipality, safety surfacing manufacturer.

After which, Unity Creations, Ltd. / Unity Surfacing Systems products shall be installed as specified using the “step-&-repeat” system to stagger (zigzag) the seams as if you would install “brickwork”, lining real seams up with fake seams. Adhesive shall be applied to the interlocks (both inside the interlocking joints and on top) and sub-base, especially the corners of each product being installed to the sub-base. Screw-bolts shall be applied through the male interlocks and counter-sunk at least two (2”) inches into the solid sub-base material. Playground posts, etc., shall be cut and aligned as required to fit without any gaps. Said cuts shall be on a 30-degree angle to allow for glue to maintain on the cut unit for added adhesion. Unity Creations, Ltd. / Unity Surfacing Systems products shall be installed utilizing full units only leaving all “male” interlocks exposed to later accept the bordering system that will be installed. The installation manual / guide shall also be read in full by the General Contract’s foreman and all parties of the installation crew.

* Base gluing (glue-down) and screw-bolts do not apply to rooftop installations. Glue being applied to the interlocks, both in the joint and on top of the joint, shall be maintained.

4.02 MEASUREMENTS AND PAYMENTS

The quantity of tiles/mats/blocks/pavers, black or colored of various drop heights/thicknesses to be paid for under these items shall be the number of units of safety surfacing material furnished and installed in accordance with the plans, specifications and directions of the Architect/Engineer.

The price bid shall be the unit price per square foot of tiles/mats/blocks of each drop height and shall include the cost of all labor, materials and incidentals necessary to complete the work, including all submittals and all necessary adhesive, bolts, in accordance with the plans and specifications, to the satisfaction of the Architect/Engineer. No deduction shall be made for cut surfacing removed for cross section of posts or any boarding system.

END OF SECTION 02791