SECTION 32 18 16.33

PLAYGROUND PROTECTIVE SURFACING

Splash Design, Four (4.0”) inches thick, yielding a twelve (12’) foot fall rating.

PART 1:	GENERAL

  - Section Includes:

Resilient, self-interlocking (with “Button-Lock™ Technology”) unitary, rubberized safety surfacing, flooring and paver products in the tile/mat/block/paver form with bolt-down capabilities, known as the: Splash Design, 4.0” thick “XL” Series offering shock resistance/impact attenuation.

  - Related Sections:

Division 32

Sub: 32 18 00 Athletic and Recreational Surfaces.

Specifically; 32 18 16 Synthetic Resilient Surfaces.

Specifically; 32 18 16.33 Playground Protective Surfacing.

Specifically; 32 18 23 Athletic Surfaces.

Division 9

Sub: 09 65 00 Resilient Flooring.

Specifically: 09 65 19 Resilient Tile Flooring.

Specifically: 09 65 19.33 Rubber Tile Flooring.

Specifically: 09 65 66 Resilient Athletic Flooring.

Division 11

Sub: 11 68 00 Playfield Equipment and Structures.

Specifically; 11 68 13 Playground Equipment.

Specifically: 11 68 16 Play Structures.

  - References

- Applicable Standards:

American Standard for Testing Materials (ASTM)

Consumer Product Safety Commission (CPSC)

American National Standards Institute (ANSI)

Factory Mutual (FM)

- ASTM F1292-04 and F355-95 Drop Test:

Standard Test Method for Impact Attenuation of Surface Systems Under and Around Playground Equipment.

- ASTM C67 Weathering/Aging:

Standard Test Method for Weathering and Aging of Surface Systems and Materials.

Standard Test Method for Rubber – Deterioration in an Air Over.

- ASTM E108: Class A Fire Test/Flammability:

Standard Test Method for Fire Tests of Surface Systems and Materials.

- ASTM E108 Class A Fire Test/Flammability - Modified for Roof Coverings:

Modified Test Methods for Fire Tests of Roof Covering Materials.

- ASTM D2859 Burn Pill:

Standard Test Method for the Surface Flammability of Products (Burn Pill Test).

- ASTM E303-93 (2013) Skid Resistance:

Standard Test Method for Measuring Surface Frictional Properties Using the British Pendulum Tester.

- ASTM F1951-99 ADA Accessibility:

Standard Specification for Determination of Accessibility of Surface Systems Under and Around Playground Equipment.

I.) CPSC-CH-E1002-08 Lead Content:

LEAD Test - For compliance with US Public Law 110-314 (HR 4040 “Consumer Product Safety Improvement Act of 2008”), lead in accessible substrate materials.

J.) Water Penetration Test:

For compliance with Sustainable Storm Water Run-off in a testing environment to determine how much water flows through the product based on real world scenarios.

K.) Leadership in Energy and Environmental Design (LEED):

1.) Criteria development by the United States Green Build Council (USGBC):

a.) Materials and Resources:

Up to 6 points / credits toward LEED certification.

b.) Indoor Environmental Quality:

Up to 1 point / credit toward LEED certification.

L.) UL 2218, Class 4 Impact Resistances, 2010:

Standard Test Method for Impact Resistance of Prepared Roof Covering Materials.

M.) ASTM D 412(13) Tensile Strength, Elongation at Break and Modulus:

Standard Test Methods for Vulcanized Rubber and Thermoplastic Elastomers – Tension.

N.) ASTM D 624 Tear Resistance:

Standard Test Method for Tear Strength of Conventional.

O.) ASTM D 3389 (10) Taber Abrasion Index:

Standard Test Method for Walking Surface Based on Abrasion Cycles.

P.) ASTM D 2240 Durometer Hardness:

Standard Test Method for Measuring the “Hardness” of Rubber Elastomers and Plastic.

Q.) ASTM D 1667 Compression Deflection:

Standard Test Method for Flexible Cellular Materials.

R.) ASTM E-831 Coefficient of Thermal Expansion:

Standard Test Method for Thermal Expansion of Materials by Thermomechanical Analysis

S.) ASTM D 3574 Compression Resistance:

Standard Test Method for Flexible Cellular Materials.

T.) ASTM D 3676 (13) and D 395 Mass and Density Per Unit Area, including Compression Set:

Standard Specification for Rubber by way of Mass, Density and Recovery Per Area.

U.) Tensile Strength at Interlocking Joint:

For compliance with Pull Force in a testing environment to determine how much pressure it takes to unlock the interlocking joints based on real world scenarios.

1.4 Submittals:

A.) General:

1.) Submit listed submittals in accordance with Conditions of the Contract and Division pertaining to Submittal Procedures Section.

B.) Product Data:

1.) Submit manufacturer’s product data, specifications, detailed drawings and installation

Instructions, as well as manufacturer’s maintenance and cleaning instructions.

C.) Verification Samples:

1.) Submit manufacturer’s standard verification samples of 4”X4” minimum. Two of the submitted samples must show the male/female self-interlocking connection (with “Button-Lock™ Technology”), Bolt-down capabilities and Glue Reservoir channel.

D.) Manufacturers Project References:

1.) Submit reference list of at least 20 years of projects in all sizes, types and scopes.

2.) Include project name, location and contact person of three (3) projects that are similar in size, type and scope as specified herein.

E.) Installer’s Project References:

1.) Submit a copy of manufacturers issued installation warranty certification.

2.) Installers must have 5 years’ experience with projects of similar scope & complexity.

`		F.) Closeout Submittals: Submit the following:

1.) Warranty documents as specified herein.

2.) Repair & Maintenance documents as issued by the manufacturer.

3.) Photographs of completed installation, with close-up shots of cut tiles.

4.) Submit listed “Closeouts” in accordance with Conditions of the Contract and Division pertaining to Closeout Procedures Section.

- Approvals:

- Contact manufacturer for information on approvals by major owners, agencies, architects, engineers, municipalities and other industry entities.

- Environmental Considerations:

- These resilient, rubberized safety surfacing flooring and paver products in the tile/mat/ block/paver form makes extensive use of clean recycled tire rubber and other recycled rubber products as a major component of its operation that are sourced/recycled in the United States of America.

- Testing Data Results:

1.) Submit certified test reports from qualified independent testing agency indicating

results of the following testing:

a.) Applicable Standards (ASTM, CPSC, ANSI, FM).

b.) Impact Attenuation (ASTM F1292-04 & F355.95)

c.) Weathering/Aging (ASTM C67, D573 & F1292-04)

d.) Flammability/Fire Test (ASTM E108)

e.) Flammability (ASTM E108 Modified for roof covers)

f.) Flammability/Burn Pill Test (ASTM2859)

g.) Skid Resistance (ASTM E303-93 / 2013)

h.) ADA Accessibility (ASTM F1951-99)

i.) Lead in Materials/Children’s Products (CPSC-CH-E1002-08)

j.) Water Penetration Test (Sustainable Storm Water MGT/Run-off)

k.) Leadership in Energy and Environmental Design (LEED)

l.) Class 4 Impact Resistance (UL 2218, 2010)

m.) Tensile Strength, Elongation at Break and Modulus (ASTM D 412)

n.) Tear Resistance (ASTM 624)

o.) Taber Abrasion Index (ASTM D3389)

p.) Durometer Hardness (ASTM 2240)

q.) Compression Deflection (ASTM 1677)

r.) Coefficient of Thermal Expansion (ASTM 831)

s.) Compression Resistance (ASTM 3574)

t.) Mass & Density (ASTM 3676) with Compression Set (ASTM D395)

u.) Tensile Strength at Interlocking Joint (Pull Force)

  - Quality Assurance/Control:

- Manufacturers Qualifications: Manufacturer shall meet a minimum of one (1) of the following two (2) criteria:

- Consistently engaged in manufacturing of self-interlocking rubber tiles/mats/blocks/ pavers of similar type that is specified, with a minimum of fifteen (15) years of experience under the same business name and EIN (Employer Identification Number)

- Furnished/Supplied a minimum of ten-million (10,000,000) square feet of self-interlocking rubber tiles/mats/blocks/pavers of similar type that is specified.

B.) Installers Qualifications:

1.) Installers must have 5 years’ experience with projects of similar scope & complexity.

2.) Certificate of qualifications from the product installer verified by manufacturer.

1.6 Delivery, Storage and Handling

A.) Delivery:

1.) All materials shall be delivered in good condition in its original unopened packages, bound and shrink wrapped with all labels intact clearly identifying manufacturer, product series/name, color and type.

B.) Storage:

1.) All materials and accessory items shall be protected from weather; and shall be stored at temperatures of 40 degrees Fahrenheit (4 degrees C) and rising for 24-hours min.

2.) Protect all materials and accessory items from direct sunlight before and during installations.

C.) Handing:

1.) Protect all materials and accessory items during handling and installation to prevent unnecessary damage. Product must be installed daily until finished.

1.7 Environmental Requirements

A.) Tile and Air Temperatures:

1.) Ensure both the tile and air temperature is a minimum of 50 degrees Fahrenheit (10 degrees C) and rising for 24-hours min.

2.) Consult with manufacturer’s installation guide/manual for installations in conditions less than 50 degrees Fahrenheit (10 degrees C) and/or greater that 85 degrees Fahrenheit (29 degrees C).

1.8 Warranty Information

A.) Manufacturer’s Warranty:

1.) Submit, for Owner’s acceptance, manufacturer’s standard warranty document executed by authorized company official. Manufacturer’s warranty is in addition to, and

not a limitation of, other rights Owner may have under contract documents.

a.) Material Warranty Period:

1.) Submit a standard Ten (10) Year Warranty from date of product shipment; or a Twenty (20) year Pro-rated Warranty from date of product shipment shall be selected prior to ordering. A default Ten (10) Year Pro-rated Warranty shall be issued if no other warranty is selected prior to ordering.

b.) Installation/Workmanship Warranty Period:

1.) Standard three (3) Years from date of product installation; or a Six (6) Year Pro-rated Warranty from date of product shipment shall be selected from the certified installer prior to ordering. A default One (1) Year Warranty shall be provided by the contractor directly if no other warranty is selected prior to ordering.

PART 2:	PRODUCTS

2.1 Manufacturer

A.) Unity Surfacing Systems, A Product of Unity Creations, Ltd. 3997 Route 9W (PO Box 9) Saugerties, New York 12477. Toll Free: (1-877) 41-UNITY, Phone (845) 246-2700, Fax: (845) 246-1700, E-mail: productinfo@surfacingsystems.com, Internet: www.surfacingsystems.com

2.2 Playground Protective Surfacing

A.) Description:

1.) Resilient, Self-Interlocking (w/Button-Lock™ Technology) Tile/Mat/Block/Paver size: 22” X 44” = 6.72 sq. ft. per unit (pre-cured). Cured products will measure 21.75” X 43.5” = 6.57 sq. ft. per unit.

2.) Shadow-center (fake seam) joint to achieve the use of the “step-&-repeat” system to stagger (zigzag) the seams as if you were installing brickwork, lining real seam up with fake seams.

B.) Basic Use:

1.) Designed for Athletic and Recreational use, such as, but not limited to: playgrounds, recreational, weight rooms, fitness, diving board areas, etc. Installed over poured asphalt (blacktop), concrete (cement) or compacted crushed stone substrate.

- Composition and Materials:

- Resilient, self-interlocking, compression molded, rubberized safety surfacing flooring and paver products in the tile/mat/block/paver form consists of three product families:

- Post-Consumer Black Recycled SBR (Styrene Butadiene Rubber) – recycled in-house, Splash Design top and polyurethane binding agents.

b.) Splash Design top produced using a virgin rubber chip/granule mixed at a ratio of 60% Black and 40% TPV/EPDM rubber chips/granules. Said TPV/EPDM can be mixed with Standard Black to achieve a desired color blend as specified.

c.) Raw materials are mixed using a polyurethane and molded with heat and pressure.

- Dual layer construction produced with bottom design consisting of solid cones (feet and/or legs) for maximum shock resistance/impact attenuation. Bottom design shall also allow for maximum contact between the bottom of the finished product and sub-base.

- Locking Type:

- Infinity-shaped, self-interlocking connection to lock to adjoining product.

- Product Edge Type:

- Tampered along the edge.

- Tampered down the middle of the 44” length.

- Symmetry of 22” by 22” squares will be seen on properly completed jobs/ installations.

#### F.) Thickness and Weights:

1.) 4” (4.0”) thick “XL” series shall be ~54 lbs. each/~8 lbs. per sq. ft.

yielding a twelve (12’) foot fall protection rating.

- Wear Layer:

- Overall - to be a minimum of one (1”) inch thick.

- Base Layer: Integral solid cone pedestal design/pattern underside forming channels for water drainage between protective tiles/mats/blocks and substrate to drainage outlet.

I.) Color:

1.) Splash Design Color (sprinkled on top of a Standard Black unit):

a.) Splash Design: Mixed at a ratio of 60% Black and 40% TPV/EPDM.

b.) Color Selection(s): Red (Terra Cotta), Brt. Red, Green, Brt. Green, Dark Green, Blue, Lt. Blue, Azure Blue (Teal), Purple, Lt. Purple, Turquoise, Beige, Eggshell (Cream), Brown, Dark Brown, Mustard Yellow, Brt Yellow, Orange, Dark. Gray, Mid-Gray, Lt. Gray, Virgin Black.

NOTE: Specifier can select multiple Splash Designs, Pigmented and Solid TPV Top colors that may be used for this project based on designs, layouts and patterns as indicated on the drawings.

- Critical Fall Height Requirement:

- Shall yield a twelve (12’) foot fall protection rating.

K.) Testing Data Results:

1.) Shock Attenuation (ASTM F1292-04 & F355.95):

a. G-max Score – Less than 200: Passing a 12’ (foot) fall rating at 4.0” thick.

b. Head Injury Criteria (HIC) Score – Less than 1000: Passing a 12’ (foot) fall rating at 4.0” thick.

2.) Weathering/Aging (ASTM C67, D573 & F1292-04):

a. G-max – Less than 200: Passing a 12’ (foot) fall rating at 4.0” thick.

b. Head Injury Criteria – Less than 1000: Passing a 12’ (foot) fall rating at 4.0” thick.

c. Rubber Deterioration in an Air Over (ASTM D573): No Deterioration found.

- Flammability/Fire Test (ASTM E108):

  - CLASS “A” FIRE RATING = Passes.

- Flammability (ASTM E108 Modified for roof covers):

  - CLASS “A” FIRE RATING = Passes from the underside of the product.

- Flammability/Burn Pill Test (ASTM2859):

  - NO OFF GASSING @ 3.7”

- Skid Resistance (ASTM E303-93 / 2013):

- Dry = 80.25. Passed.

- Wet = 67. Passed.

- ADA Accessibility (ASTM F1292-99):

a. Firmness = 0.26. Passed.

b. Stability = 0.28. Passed.

8.) Lead in Materials/Children’s Products (CPSC-CH-E1002-08):

a. NOT DETECTED

9.) Water Penetration Test (Sustainable Storm Water MGT/Run-off):

a. BODY = Penetration is .13 Gallons Per Minute, Per Square Foot of surface area

b. SEAM = Penetration is .21 Gallons Per Minute, Per Square Foot of surface area

10.) Leadership in Energy and Environmental Design (LEED):

a. Criteria development by the United States Green Build Council (USGBC):

i.) Materials and Resources:

Up to 6 points / credits toward LEED certification.

Recycled Content………………………...MR. 4.1

Recycled Content………………………...MR. 4.2

Local/Regional Materials…………………MR 5.1

Local/Regional Materials…………………MR 5.2

Construction Waste Mgt………………….MR 2.1

Construction Waste Mgt………………….MR 2.2

ii.) Indoor Environmental Quality:

Up to 1 point / credit toward LEED certification.

Low Emitting Materials…………………..EQ 4.1

11.) Class 4 Impact Resistance (UL 2218, 2010):

Six different drop zones observed no damage. No evidence of tearing,

fracturing, cracking, splitting, rupturing, crazing, or other evidence of

opening of the rubber paver system = Passed.

12.) Tensile Strength, Elongation at Break and Modulus (ASTM D 412), [MPa] & [%]:

a. Tensile Strength: 0.87 MPa

b. Tensile Strength at Break: 0.76 MPa

c. Elongation: 71.5%

d. Elongation at Break: 92.4%

e. Modulus: 3.49 MPa

13.) Tear Resistance (ASTM 624), [N] & [kNm]:

a. Peak Tearing Load: 156 N

b. Peak Tearing Strength: 11.3 kNm

14.) Taber Abrasion Index (ASTM 624): 0719 WC

15.) Durometer Hardness (ASTM 2240): Shore A = 54

16.) Compression Deflection (ASTM 1677): 577 kPa @ 25%

17.) Coefficient of Thermal Expansion (ASTM 831): 0013 in/ft. per degree

18.) Compression Resistance (ASTM 3574), [kN] & [kPa]:

a. Load at Preset point: 2.78 kN

b. Compression Resistance:1030 kPa

19.) Mass & Density (ASTM 3676), psf & pcf/kg/m3

a. Mass Per Area: 2.92 psf

b. Density Per Area: 78.8 pcf/1282 kg/m3

c. Recovery (D395): 90-100% w/No Cracking

20.) Tensile Strength at Interlock Joint (Pull Force to Separate Interlock), two directions:

a. Vertical Pull Force Test: 127 PSI or Greater.

b. Horizontal Pull Force Test: 38 PSI or Greater.

2.3 Accessories Items:

A.) Unity’s Chemrex 948 Urethane Adhesive (Large Tubes):

1.) For gluing interlock-to-interlock adhesion, both inside the joint (inside wall) and outside the joint (outside edge) as well as product-to-solid sub-base installations (gluing the underside cones/feet/legs outside edge of each unit being installed).

- Unity’s Transitional Ramp, Standard Beveled Edge:

- For above grade installations. Slope is standard at 22”.

- Pales of adhesive/glue shall be used on installations that require transitional ramps/ edges.

- Unity’s Geotextile Fabric, Landscaping Mesh.

- Shall only be used over loose-filled, ground level, installation.

- Fabric/Mesh shall be cut away from any and all drains accordingly.

- Unity’s Anchor Bolts (bolt-down installations):

- Shall be used for solid sub-base ground level installations only. DO NOT USE ON ROOFTOP APPLICATIONS WHAT-SO-EVER.

PART 3:	EXECUTIONS

3.1 Examinations/Inspections

A.) Prior to application of the safety surfacing, flooring and paver products, the architect, engineer, municipality, general contractor, safety surfacing manufacturer/representative and installer shall evaluate the substrate’s structural performance. Notify all parties of all displacements or stress cracks.  Work shall not proceed until unsatisfactory conditions are corrected and signed by all parties; And manufacturers installation manual/guide has been read.

3.2 Preparations:

- Do not proceed with safety surfacing, flooring and/or paver installation until all applicable site work, including substrate/sub-base preparation, fencing, playground equipment installation and all other relevant work, has been fully completed and approved prior to commencement of safety surfacing, flooring and paver products. Verify that substrate conditions are suitable for installation of the safety surfacing, flooring and pavers; and do not proceed with installation until unsuitable conditions are corrected, verified and approved.

- Variations in Elevations: Shall repair variations in elevation of sub-base surfaces greater than +/- one-quarter (1/4”) inch over ten (10) feet in any direction.

3.3 Installations:

A.) The installation manual / guide shall also be read in full by the General Contract’s foreman

and all parties of the installation crew.

- Tiles/mats/blocks/pavers as well as sub-base material shall be clean and dry for a minimum of 24-hours prior to installation.

- Tiles/mats/blocks/pavers shall be installed in accordance with manufacturer’s specific installation instructions at any and all locations as indicated on the Drawings.

- Tiles/mats/blocks/pavers shall be installed on a rectangular configuration of 22” (inches) by 44” (inches) in size [+/- quarter (1/4”) tolerance] with a shadow-center (fake seam) joint to achieve the use of the “step-&-repeat” systems to stagger the seams as if you were installing brickwork (zigzag). As a result, symmetry of 22” by 22” squares will be seen on properly completed jobs (installations).

E.) Adhesive shall be applied in accordance with the manufacturers specific installation instructions for interlock-to-interlock (both inside the joint – back wall, and outside edge of interlocking joint in order for glue to ooze throughout the interlocking system), as well as product-to-solid sub-base installations. Such application will allow for proper rainwater drainage.

H.) Maintain a straight line at the product’s real seams (usually horizontal). To keep lines straight, adjust products using a rubber mallet as they are installed. Apply a string line on the first couple of rows installed to maintain a straight line throughout. Repeat string-line process every so often to make sure you continue a straight line/run of installed products.

I.) Screw-bolts shall be applied through the male interlocks and counter-sunk every 22” inches into the solid sub-base material. DO NOT USE SCREW-BOLTS ON ROOFTOPS.

J.) All posts and protrusions, etc., shall be cut and aligned as required to fit without any gaps.

Said cuts, including lead-in cuts, shall be on a 30-degree angle to allow for glue to maintain on

the cut unit for added adhesion.

K.) Precautions:

1.) Remove adhesive (glue) spills from installation area using a clean dry rag and mineral spirits in accordance with manufacturer’s installation guide/manual.

- If applicable, cut geo-textile fabric/landscaping mesh away from any and all drains. Do not cover drains, drain covers, drainage outlets what-so-ever.

3.4 Field Quality Control:

A.) Prior to installation, Contractor shall provide the architect of record and the owner a signed copy of the “Installation Warranty” in writing prior to installation commencement.

B.) Contractor shall “certify” in writing that the sub-base material(s) have been properly compacted, cured and dry as per the Section pertaining to sub-base, prior to installation.

C.) Contractor shall “certify” in writing that the “Installation Guide/Manual” has been read by Project Manager, by the Lead Installer and Installation Crew prior to installation commencement.

3.5 Protection

A.) Protect the installation area from any and all types of subsequent construction and/or foot traffic whether it is human, animal or machine for a minimum of twenty-four (24) hours after installation has occurred.

END OF SECTION 32 18 00 (02791)

Specifiers Notes:

Introduction:

This specification product guide is written according to the Construction Specification Institute (CSI) and the Construction Specifications Canada (CSC) 3-Part Format, MasterFormat, SectionFormat and PageFormat, as described in The Project Resource Manual – CSI Manual of Practice (April 2016 Edition).

The Section(s) must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building code requirements. Coordinate the related Section(s) with other specifications section(s) and the Drawings accordingly. Delete all Specifiers Notes when editing.

1.1 Section Includes:

This covers Unity’s XL Series of resilient, unitary, rubberized safety surfacing, flooring and paver products in the tile/mat/block/ paver form. Contact Unity for assistance in editing any of these Sections for a specific application.

1.2 Related Sections:

Edit the list of related Section(s) as required for the project. List other Section(s) with work directly related to this Section(s).

Include the Section(s) number(s) and title(s) of the Division(s) Section(s), if they are referenced in this section.

1.3 References:

List standards referenced in this Section(s), complete with designation(s) and title(s). This article does not require compliance with standards, as it is simply a listing of those used.

Unity does offer the following (based on application and circumstances:

ASTM E-648, Self-Extinguishing Fire/Flammability Test: Is a value-added service that must be clearly specified, noted in the bidding process and addressed with Unity prior to ordering.

ASTM C518-98 Insulation/R-Values: Standard Test Method for Steady-State Thermal Transmission Properties by Means of the Heat Flow Meter Apparatus. Measuring = Insulation/R-Values.

ASTM E903, E891, E1980 Solar Reflectance: Hemispherical Spectral Reflectance and Total Emittance Test. Presents results of spectral reflectance and total emittance of products tested.

Leadership in Energy and Environmental Design (LEED): Shall be edited accordingly based on the criteria and location of final installation.

ASTM D 3161-09 Non-Adhered, Over-Top and at Kick-Plate) Modified for Rubber Pavers: Standard Test Method for Wind Resistance (Fan-Induced) via air velocity of 150 MPH.

  - Submittals

Include any ASTM standard herein when referencing it from 1.3 References noted above.

1.8 Warranty Information:

Refer to conditions of the overall Contract for project warranty provisions. Specifier MUST select one from type of warranty from each section.

2.1 Manufacturer:

If a local representative is to be the key contact for questions and/or pricing on a local level, their company name, contact person information, address, phone number and e-mail address should be included herein.

2.2 Playground Protective Surfacing:

It is strongly encouraged to avoid the use of transitional ramps and counter-sink the area

in question to provide ADA access at ANY and ALL points.

If needed, Transitional Ramp Edge size: 22” X 44” (slope can be found in the 22”). Cured products will measure 21.75” X 43.5” = 6.57 sq. ft. per unit and shall be specified accordingly.

I.) Testing Data Results:

Specify Test Results in accordance with project details accordingly.

Actual test reports, additional testing and additional product information are available upon written request for projects outside the norm of this specification herein.

3.2 Preparations:

Due to the Porosity of the Unity products, it is essential that a proper sub-base drainage system/run-off be used/constructed or else the products may not stay level and become damaged due to up-lift and/or shifting.

Recessed installations are strongly encouraged to avoid the use of transitional ramps (edging) as this will allow for the entire area to be ADA accessible and not just one ramp/zone/area. It is both helpful and advised to plan accordingly when preparing for a counter-sunk installation.

Crushed Stone Base – Ensure materials, compaction, thickness, slope and settling times are clearly specified. Crushed Stone Base: Shall be 3-5” thick (depending on application and use). Contractor shall prepare a compacted level sub-grade using a “stone blend” material. Stone base shall be uniformly mixed on a mixing table or by other mechanical means (such as quarry blending operations) prior to placement on the compacted earth surface sub-grade. Stone base shall be bladed and evenly compacted and shall be a minimum of five (5”) inches deep at all locations. Stone base shall be wetted during mixing operations if necessary for proper blending. Moisten and compact with a flat plate vibratory compactor to 95% proctor. Tolerance: 1/4” in any 10ft. direction. Ensure stone base is a minimum of fifteen (15) days old. Moisten and compact again if necessary. A Landscaping Fabric/Mesh shall be installed prior to finished products being applied.

Concrete Sub-base – Ensure that adhesive/glue will be used on the underside, outside edge, of each unit being installed. Concrete Sub-base: Shall be as specified in the Division pertaining to the appropriate Section. Apply a light broom finish to “lightly rough” the concrete sub-base. Ensure concrete is sound with no loose materials or cracks over 1/8” (inch) wide in size. Ensure concrete is a minimum of ten (10) days old. Test concrete for any moisture in accordance with manufacturer’s installation guide/manual to ensure it has successfully and sufficiently cured and is dry. Existing concrete sub-bases shall be pressure washed and dried in accordance with manufacturer’s installation guide/manual.

Asphalt Sub-base – Ensure that adhesive/glue will be used on the underside, outside edge, of each unit being installed. Asphalt Sub-bases: Shall be as specified in the Division pertaining to the appropriate Section. Ensure asphalt is sound with no loose materials or cracks over 1/8” (inch) wide in size. Ensure asphalt is a minimum of fifteen (15) days old. Test asphalt for any moisture in accordance with manufacturer’s installation guide/manual to ensure it has successfully and sufficiently cured and is dry. Existing asphalt sub-bases shall be pressure washed and dried in accordance with manufacturer’s installation guide/manual. Scarify existing asphalt in accordance with manufacturer’s installation guide/manual.

3.3 Installations:

Recessed installations are strongly encouraged to avoid the use of transitional ramps (edging). The height of the finished area (i.e. concrete/asphalt walkway, edging, wood, etc.) and the sub-base material shall be consistent with the thickness of the tiles/mats/blocks/pavers being installed all the way around the entire installation area, prior to the installing the Unity products. This shall be tested every 44” with a full-size sample tile/mat/block/paver given to the contractor prior to commencement of installation.

For recessed installations with a boarding system, apply adhesive to the sides of either the edging, or the products themselves at a rate of approximately 50 linear feet per 825 ml tube.

Rooftop installations, Crushed Stone sub-base and temporary installations often call for adhesive to be applied to the interlocks only. In these cases, do not apply adhesive directly onto the roofing membrane or solid sub-base materials that are temporary without consulting an engineer, architect or end-user. Yield per tube will increase to 80 sq. ft. per tube.

D.) When using gallon pales for transitional ramps, yield is 50 sq. ft. per gallon.

3.4 Field Quality Control:

D.) Contractor shall “certify” in writing that the flush test (if applicable) has been completed and verified with photographic images sent to the: architect, engineer, municipality, safety surfacing manufacturer.